- TECHNICAL DATA SHEET

- AA59588 Class 2 Sheeting Grade Silicone Rubber

- Grade: ASil 60

- Temperature Range: -60C to 200C

MECHANICAL PROPERTIES

|  |  | ###### ASil 60 |  |  |
| --- | --- | --- | --- | --- |
| Property | Units | Specification Limits | Typical Value | Test Method |
| Hardness | Shore A | 60 5 | 56 | ASTM D 2240 |
| Tensile Strength | MPa | 4.48 min | 8.88 | ASTM D 412 |
| Elongation to Failure | % | 2A – 150 min 2B – 100 min | 429 | ASTM D 412 |
| 1/Compression Set | % | 2A – 35 max 2B – 25 max | 18.1 | ASTM D 395 |
| 2/Hardness Change | Shore A | 10 | +5 | ASTM D 2240 |
| 2/Tensile Strength Change | % | -20 max | -9.6 | ASTM D 412 |
| 2/Elongation to Failure Change | % | -40 max | -2.3 | ASTM D 412 |
| Brittle Point | C | <-62.2 |  | ASTM D 2147 |
| 3/Volume Change | % | +5 max | -2.0 | ASTM D 471 |
| Tolerances |  | AA59588 Table VII |  |  |

Aging Period: 1/ 70 hours @ 150 C, 2/ 70 hours @ 225 C, 3/70 hours @ 100 C water immersion

Greenbank Business Park, Blakewater Road, Blackburn, Lancashire, BB1 3HU England

Telephone: +44(0)1254 261321 Facsimile:+44(0)1254 583519     Web:  www.silicone.co.uk

This information and our technical advice, whether verbal, in writing or by way of trials, is given in good faith but without warranty.  This also applies where proprietary rights are involved.  Our advice does not release you from the obligations to check its validity and to test our products as to their suitability for the intended use.  The storage, application and use of our products are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with our General Conditions of Sale. The information contained within this data sheet is subject to change without notice