TECHNICAL DATA SHEET

Cellular Silicone Elastomer

Grades: AMS 3195 & AMS 3196

Temperature Range: -103F to 205F

AVAILABILITY

These grades of cellular silicone elastomers have been specially formulated to meet the SAE AMS 3195E and AMS 3196F specifications. The range is available as sheeting, profile extrusions, jointed rings, self-adhesive backed, strip and punchings. They are particularly suited to use in applications that require a closed-cell sponge rubber that remains flexible over a wide temperature range. There is a full range of standard colours available and Silicone Engineering has the capability to colour match to customer requirements. Sheeting is available in a standard width of 3 foot; other widths can be produced upon request.

SPECIFICATIONS

SAE AMS 3195E Sponge, Silicone Rubber Closed Cell, Medium

SAE AMS 3196F Sponge, Silicone Rubber Closed Cell, Firm

These products meet the flammability requirements of FAR 25.853 (a)(1)(iv) and (a)(1)(v) horizontal flammability tests.

GENERAL CHARACTERISTICS FOR SILICONE RUBBER

| Limiting Oxygen Index | 23.2 % | BS 2872 Part 1 |
| --- | --- | --- |
| Thermal Conductivity | 6.4x10-2 W.m-1.K-1 | BS 874 Part 2 |
| Radiation Resistance | >105 Grays (107 Rads) typical |  |

MECHANICAL PROPERTIES

|  | ###### AMS 3195 |  | ###### AMS 3196 |  |  |
| --- | --- | --- | --- | --- | --- |
| Property | Specification Limits | Typical Value | Specification Limits | Typical Value | Test Method |
| Density (lb.in-3) | 0.025 max. 0.020 max. | #0.019 0.010 | 0.030 max. 0.025 max. | *0.024 0.017 | ASTM D1056 < 0.25” >0.25” |
| Compression Stress (psi) 25% strain | 6 – 14 | 7.3 | 12 –20 | 18.0 | ASTM D1056 |
| Compression Set (%) 22 hours @ 212°F | 60 max. | 3.8 | 60 max. | 5.7 | ASTM D1056 |
| Brittleness Temperature (F) | -67 max. | -112 | -67 max. | -112 | ASTM D746 |

*0.079” sample

#0.118” sample