- TECHNICAL DATA SHEET

- Commercial Grade Silicone Rubber Sheeting

- Grades: ESil 50,60,70 and 80

- Temperature Range: -60C to 200C (-76°F to 392°F)

MECHANICAL PROPERTIES

|  |  | ESIL 50 | ESIL60 | ESIL70 | ESIL80 |  |
| --- | --- | --- | --- | --- | --- | --- |
| Property | Units | Specification Limits | Specification Limits | Specification Limits | Specification Limits | Test Method |
| Hardness | Shore A | 50 5 | 60 5 | 70 5 | 80 5 | ASTM D2240 |
| Tensile Strength | MPa PSI | 5.0 min 725 min | 5.0 min 725 min | 4.0 min 580 min | 4.0 min 580 min | BS903 A2 ASTM D412 |
| Elongation to Failure | % | 200 min | 200 min | 200 min | 200 min | BS903 A2 ASTM D412 |
| Tear Strength | N.mm-1 lb.in-1 | 8.0 min 45.7 min | 8.0 min 45.7 min | 8.0 min 45.7 min | 8.0 min 45.7 min | BSISO 34-1 ASTM D624 |
| Compression Set 24 Hours @ 150°C/300°F | % | 50 max | 50 max | 50 max | 50 max | BS 903 A6 ASTM D395 |

Greenbank Business Park, Blakewater Road, Blackburn, Lancashire, BB1 3HU England

Telephone: +44(0)1254 261321 Facsimile:+44(0)1254 583519     Web:  www.silicone.co.uk

This information and our technical advice, whether verbal, in writing or by way of trials, is given in good faith but without warranty.  This also applies where proprietary rights are involved.  Our advice does not release you from the obligations to check its validity and to test our products as to their suitability for the intended use.  The storage, application and use of our products are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with our General Conditions of Sale. The information contained within this data sheet is subject to change without notice