TECHNICAL DATA SHEET

Cellular Silicone Elastomer

Grades: SE515 & SE 524

Temperature Range: -76F to 392F

AVAILABILITY

The SE range of cellular silicone elastomers are available as sheeting, profile extrusions, jointed rings, self-adhesive backed, strip and punchings. They are particularly suited to use in high temperature seals and gaskets, where a soft, easily deformed rubber is required. There is a full range of standard colours available and Silicone Engineering has the capability to colour match to customer requirements. Sheeting is available in standard rolls of width 3 foot; other widths can be produced upon request.

SPECIFICATIONS

These products meet the flammability requirements of FAR 25.853 (a)(1)(iv) and (a)(1)(v) horizontal flammability tests.

GENERAL CHARACTERISTICS FOR CELLULAR SILICONE ELASTOMER

| Brittle Point | -112F | ASTM D746 |
| --- | --- | --- |
| Limiting Oxygen Index | 23.2 % | BS 2872 Part 1 |
| Thermal Conductivity | 6.4x10-2 W.m-1.K-1 | BS 874 Part 2 |
| Radiation Resistance | >105 Grays (107 Rads) typical |  |

MECHANICAL PROPERTIES

|  | ###### SE515 |  | ###### SE524 |  |  |
| --- | --- | --- | --- | --- | --- |
| Property | Specification Limits | Typical Value | Specification Limits | Typical Value | Test Method |
| Density (lb.ft-3) | *12.1 – 19.0 #22.5 – 31.1 | 15.6 27.6 | *22.5 – 27.6 #31.1 – 38.0 | 24.2 34.6 | ASTM D1056 |
| Compression Stress (psi) 25% strain | **0.5 – 12 | 6.15 | **4.0 – 15.5 | 9.5 | ASTM D1056 |
| Compression Set (%) 22 hours @ 160°F | 60 max. | 20 | 60 max. | 15 | ASTM D1056 |

*Measured on 1” diameter cord sample

#Measured on 0.125” sample

**Measured on 0.5” sample, on thinner samples typical value will be higher than published here.

For further information about the physical properties of these materials, contact the technical department.