TECHNICAL DATA SHEET

Flame Retardant Silicone Rubber

Grades: SE40FR SE50FR SE60FR SE70FR & SE80FR

Temperature Range: -60C (-76F) to 230C (446F)

AVAILABILITY

The SE range of Silicone Rubbers is available in the form of mouldings and profile extrusions, which can be jointed or self-adhesive backed. SE 60 FR is also available as sheeting. They are particularly suited to use as seals and gaskets, in areas where public safety is critical.  There is a full range of standard colours available and Silicone Engineering has the capability to colour match to customer requirements.

**Other materials available at silicone engineering include solid sheeting, sponge sheeting, sponge extrusion, customer compounding and cable grades**

SPECIFICATIONS

Translucent, White, Blue and Red Iron Oxide variants contain only ingredients that are listed by the American Food and Drugs Administration (FDA) under the 21 CFR number 177-2600.

These products meet the flammability requirements of FAR 25.853 (a)(1)(i), (a)(1)(ii) vertical and (a)(1)(iv), (a)(1)(v) horizontal flammability tests.

They also meet the requirements of UL94 V0, V1, and V2. However, these materials do not hold UL approval.

GENERAL CHARACTERISTICS FOR SILICONE RUBBER

| Brittle Point | -80C (-112 F) | ASTM D746 |
| --- | --- | --- |
| Limiting Oxygen Index | 24.0 % | BS 2872 Part 1 |
| Thermal Conductivity | 0.24 W.m-1.K-1 | VDE 0304 |
| Radiation Resistance | >105 Grays (107 Rads) typical |  |
| Dielectric Strength | 23 kV.mm-1 | VDE 0303 |
| Dielectric Constant | 2.9 | VDE 0303 |
| Dissipation Factor @ 50c/s | 3x10-4 | VDE 0303 |
| Volume Resistivity | 3x1015 .cm | VDE 0303 |

Environmental Resistance – Silicone rubber products have an excellent resistance to ozone, oxidation, ultraviolet light, corona discharge, cosmic radiation, ionising radiation and weathering in general. Typical radiation resistance is > 105 grays (>107 rads)

MECHANICAL PROPERTIES

|  |  | #### SE40FR |  | ###### SE50FR |  | SE60FR |  | ###### SE70FR |  | ##### SE80FR |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Property | Units | Specification Limits | Typical Value | Specification Limits | Typical Value | Specification Limits | Typical Value | Specification Limits | Typical Value | Specification Limits | Typical Value | Test Method |
| Hardness | Shore A | 40 5 | 43 | 50 5 | 52 | 60 5 | 62 | 70 5 | 72 | 80 5 | 80 | ASTM D2240 DIN 53505 |
| Tensile Strength | MPa psi | 4.0 min. 580 min. | 6.5 943 | 5.5 min. 798 min. | 7.5 1088 | 5.5 min. 798 min. | 8.0 1160 | 6.0 min. 870 min. | 9.1 1320 | 6.0 min. 870 min. | 8.4 1218 | BS 903 pt A2 DIN 53504 die S1 ASTM D412 die C |
| Elongation to Failure | % | 300 min. | 450 | 250 min. | 330 | 250 min. | 300 | 200 min. | 280 | 200 min. | 250 | BS 903 pt A2 DIN 53504 die S1 ASTM D412 die C |
| Tear Strength | N/mm lb/in | 8.5 min. 48.5 min. | 12.0 85.6 | 10.0 min. 57.1 min. | 15.0 102.8 | 12.5 min. 71.4 min. | 15.0 102.8 | 12.5 min. 71.4 min. | 14.0 97.1 | 10.0 min. 57.1 min. | 12.5 91.3 | BSISO 34-1 Method C ASTM D624 die C |
| Compression Set 24 hours @ 150°C 22 hours @ 300°F | % | 30 max. 30 max. | 25 22 | 30 max. 30 max. | 14 12 | 30 max. 30 max. | 10 10 | 30 max. 30 max. | 12 11 | 30 max. 30 max. | 16 17 | BS 903 pt A6 type B DIN 53517 type II ASTM D395 method B type 2 |

*other information regarding the physical properties of these materials is available on request