TECHNICAL DATA SHEET

Flame Retardant Cellular Silicone Elastomer

Grades: SE510FR UL94V0 & SE515FR UL94V0

Temperature Range: -76F to 392F

AVAILABILITY

The FR range of cellular silicone elastomers are available as sheeting, profile extrusions, jointed rings, self-adhesive backed, strip and punchings. They are particularly suited to use in high temperature seals and gaskets, where a soft, easily deformed rubber is required and where public safety is critical. Sheeting is available in standard rolls of width 1m and length 10m; other widths or lengths can be produced upon request. The scope of the UL approval for these products limits the minimum dimensions and colours that can be manufactured, for further information please contact the Silicone Engineering sales team.

SPECIFICATIONS

These products have been specifically formulated for and hold approval to the flammability requirements of the UL94 V0 specification. The UL file number for these materials is E235077. As V0 is the most demanding of the UL94 vertical burn tests, these grades may also be used in applications where V1 or V2 rating is required.

MECHANICAL PROPERTIES

|  | ###### SE510FR UL94 V0 |  |  | SE515FR UL94 V0 |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Property | Specification Limits | Typical Value | Specification Limits |  | Typical Value | Test Method |
| Density (lb.ft-3) | 10.0 1.9 22.5 3.7 | 10.6 19.4 | 13.7 1.9 25.0 3.7 |  | 13.6 25.2 | BSENISO 845 *1.0 inch sample *0.12 inch sample |
| Compression Stress (lb.in-2) 40% strain | 4.4 2.9 | 2.0 | 10.2 2.9 |  | 9.9 | BSENISO 3386 part 1 *1.0 inch sample |
| Compression Set (%) 24 hours @ 158°C | 20 max. | 12 | 15 max |  | 10 | BSENISO 1856 Type A |

*The density of sponge varies with the thickness of the product. As the thickness decreases the density increases in addition as the density increases the stiffness of the product increases. For more information relating to the apparent density of any specific thickness and what affect this would have on performance, please contact the technical department.